PE-PVC INDOOR CABLE

Applications：

This cable is PE insulated PVC jacketed unit type quad cable, used as telephone distribution circuits inside building.

The wires of the cable are identified by the color code of insulation.

| Conductor |  | No. of pair | PVC Insulation | PVC Overall | Diameter Overall | Standard |
| --- | --- | --- | --- | --- | --- | --- |
| AWG | Diameter (mm/inch) | P | Thickness (mm/inch) | Thickness (mm/inch) | max. (mm/inch) | Length (m/ft) |
| 26 | 0.40/0.016 | 6 | 0.15/0.006 | 1.3/0.051 | 6/0.236 | 500/152.5 |
|  |  | 10 |  | 1.3/0.051 | 7/0.275 |  |
|  |  | 26 |  | 1.3/0.051 | 11/0.433 |  |
|  |  | 30 |  | 1.3/0.051 | 11/0.433 |  |
|  |  | 50 |  | 1.4/0.055 | 13/0.512 |  |
|  |  | 100 |  | 1.6/0.062 | 17/0.670 |  |
|  |  | 200 |  | 1.9/0.074 | 24/0.945 |  |
| 24 | 0.50/0.02 | 6 | 0.17/0.007 | 1.3/0.052 | 7/0.275 | 500/152.5 |
|  |  | 10 |  | 1.3/0.052 | 8/0.315 |  |
|  |  | 26 |  | 1.3/0.052 | 12/0.472 |  |
|  |  | 30 |  | 1.3/0.052 | 12/0.472 |  |
|  |  | 50 |  | 1.4/0.055 | 15/0.590 |  |
|  |  | 100 |  | 1.6/0.063 | 20/0.787 |  |
|  |  | 200 |  | 2.0/0.078 | 27/1.063 |  |

Characteristics：

| Items | Specification |
| --- | --- |
| Conductor Resistance (20℃) | 0.40mm(TC) 147.5 Ω/km max. |
|  | 0.50mm(TC) 93.5 Ω/km max. |
| Insulation Resistance (20℃,DC 100~500V/1min) | 5000 MΩ-km min. |
| Dielectric Strength | D.C. 500 V/1min or A.C. 350 V/1min |
| Capacitance (1KHz) | 100P↑ 55 nF/km Max. |