UL 10231 High Temperature Hook Up Wire

Product Description :

Construction :

Conductor: Copper Alloy or Tinned stranded copper

Conductor

Insulation

- Insulation: Fluorine resin high temperature

- Insulation Thickness: 0.06~0.09mm

- Temperature Rating: 260℃

- Voltage Rating: 30V"

- Continuous working temp Range: -65℃ ~ +260℃

- Resistant to solvents, chemicals, gasoline and radiation

- High Dielectrical Strength (70 KV/mm) permits extremely fast transmission and minimal single distortion

- Thinner insulation and small diameter, light weight, some space with more cables.

- Tough flexible resistant to crush and abrasion.

Applications :

Notebook, medical equipment, aircraft wiring harness and Twisted-pairs for High Frequency communication

| Style | Conductor |  |  | ### Insulation Thickness | Overall Diameter |
| --- | --- | --- | --- | --- | --- |
|  | AWG | Stranding No./mm | Diameter | mm | mm |
| UL 10231 | 40 | 7/0.03 | 0.09 | 0.06 | 0.21 |
|  | 38 | 7/0.04 | 0.12 | 0.06 | 0.24 |
|  | 36 | 7/0.05 | 0.15 | 0.06 | 0.27 |
|  | 34 | 7/0.06 | 0.18 | 0.06 | 0.3 |
|  | 32 | 7/0.08 | 0.24 | 0.085 | 0.41 |
|  | 30 | 7/0.10 | 0.3 | 0.08 | 0.46 |
|  | 28 | 7/0.127 | 0.38 | 0.08 | 0.54 |